## Slide 1
NDTT1
Dye Penetrant Testing (DPT)

## Slide 2
Revision/Verification Table
Rev.no | Revision Date | Revision Detail | Revised by
00 | - | - | -
Verification Table |  |  | 
Verified by |  | Muhammad Aamer Khan | 
Date |  | 20/04/2023 | 
Notes |  | - | 

## Slide 3
Introduction
Learning Objective
Training Schedule
Examination Criteria
Main Training
CONTENTS

## Slide 4
This presentation is intended to provide knowledge of what is DPT, working principle, procedure, and application of DPT.
This is a Special Module course and is mandatory for all the Trainees of Bahria Classification Society.
INTRODUCTION

## Slide 5
The objective of this training is to establish familiarization and understanding of attendees about Dye Penetrant Testing (DPT).
LEARNING OBJECTIVES

## Slide 6
The training course is scheduled for 2-3 Hours
Training Starts at
0900
Break 1
1000-1015
Training Continuation
1015-1115
Break 2
1115-1130
Training Continuation
1130-1200/1230
TRAINING SCHEDULE

## Slide 7
Total Questions: 15
Total Marks: 30
Passing Marks: 18
Total Time: 30 min
Examination Date: Within 7 working days of Training
EXAMINATION CRITERIA

## Slide 8
MAIN TRAINING

## Slide 9
Dye penetrant inspection (DPI) is type of NDT, also called liquid penetrate inspection (LPI) or penetrant testing (PT).
Liquid penetrant testing is a method that is used to reveal surface defects by bleed-out of a colored or fluorescent dye from the defect.
INTRODUCTION
This technique is used to detect casting, forging and welding defects such as cracks, surface porosity, pinhole and blow hole etc.
It is widely applied and low-cost inspection method for all non-porous materials (metals, plastics, or ceramics).

## Slide 10
Oil and whiting method used in the railway industry in the early 1900s was the first recognized use of the principles of penetrants to detect cracks.
The oil and whiting method used an oil solvent for cleaning followed by the application of a whiting or chalk coating, which then absorbed oil from the cracks revealing their locations.
HISTORY
Soon the dye was added to the liquid.
By the 1940s, dye was added to the oil used to penetrate test objects.

## Slide 11
DPT is based upon capillary action, where low surface tension fluid penetrates into clean and dry surface breaking discontinuities.
WORKING PRINCIPLE
Capillary Action:
It is the ability of a liquid to flow in narrow spaces without the assistance of, or even in opposition to, external forces like gravity.
It occurs because of intermolecular forces between the liquid and surrounding solid surfaces.

## Slide 12
Basic processing steps of DPT are as follows:
DPT PROCEDURE

## Slide 13
STEP-1: SURFACE PREPARATION
Most critical steps of a liquid penetrant inspection.
The surface must be free of oil, grease, water, or other contaminants that may prevent penetrant from entering into flaws.

## Slide 14
Once the surface has been thoroughly cleaned and dried, the penetrant material is applied by spraying, brushing, or immersing the part in a penetrant bath.
STEP-2: PENETRANT APPLICATION

## Slide 15
The penetrant is left on the surface for a sufficient time to allow as much penetrant as possible to seep into a defect.
Penetrant dwell time is the total time that the penetrant is in contact with the part surface.
STEP-3: PENETRANT DWELL

## Slide 16
  This is the most delicate part of the inspection procedure because the excess penetrant must be removed from the surface of the sample while removing as little penetrant as possible from defects.
  Depending on the penetrant system used, this step may involve cleaning with a solvent, direct rinsing with water, or first treating the part with an emulsifier and then rinsing with water.
STEP-4: EXCESS PENETRANT REMOVAL

## Slide 17
  A thin layer of developer is then applied to the sample to draw penetrant trapped in flaws back to the surface where it will be visible.
  Developers come in a variety of forms that may be applied by dusting (dry powdered), dipping, or spraying (wet developers).
Step-5: Developer Application

## Slide 18
The developer is allowed to stand on the part surface for a period of time sufficient to permit the extraction of the trapped penetrant out of any surface flaws.
This development time is usually a minimum of 10 minutes.
Step-6: Indication Development

## Slide 19
Inspection is then performed under appropriate lighting to detect indications from any flaws which may be present.
Defects are recorded.
Step-7: Inspection/Evaluation

## Slide 20
Step-8: Post Cleaning
The test surface is cleaned after inspection.

## Slide 21
Following items are used in DPT:
Cleaner/Remover
Penetrant
Developer
DPT Items

## Slide 22
The penetrants are mixtures of organic solvents, which are characterized by their ability to wet materials, spread rapidly and penetrate into defects.
These materials used today are much more sophisticated than kerosene and whiting first used by railroad inspectors near the turn of 20th century.
Today's penetrants are carefully formulated to produce the level of sensitivity desired by the inspector.
Penetrant Materials

## Slide 23
  To perform well, a penetrant must possess a number of important characteristics.
    It should spread easily over the surface being inspected.
    It should be easily drawn into discontinuities by capillary action.
    It should not be harmful to the inspector or the material being tested.
    It should possess high indicating capability & less dwell time.
    It should remain in fluid state.
    It should not affect the physical and chemical properties of the testing material.
CHARACTERISTICS OF LIQUID PENETRANTS

## Slide 24
Classification of Penetrant Materials

## Slide 25
  On the basis of their physical properties, penetrants are classified as:
  Visible Liquid Penetrants:
    They are usually red in color and produces a contrasting indication against the white developer back ground.
    They do not require a darkened area and an ultraviolet light in order to make an inspection.
    They are also less vulnerable to contamination from things such as cleaning fluid that can significantly reduce the strength of a fluorescent indication.
CLASSIFICATION ON THE BASIS OF THEIR PHYSICAL PROPERTIES

## Slide 26
  Fluorescent Penetrants:
    They are generally green in color and contain dye that glows brightly when exposed to UV lights.
    These systems are more sensitive than visible penetrant systems because the eye is drawn to the glow of the fluorescing indication.
    Dual sensitivity penetrant
    this types of penetrant combines of visible penetrant and fluorescent penetrant.
    Indication can be visible under normal light also black light.
CLASSIFICATION ON THE BASIS OF THEIR PHYSICAL PROPERTIES

## Slide 27
Each types of penetrant is again classified into 4 groups according to their removal process.
  Water Washable Penetrant
  Post Emulsifiable Penetrant - Lipophilic
  Solvent Removal Penetrant
  Post Emulsifiable Penetrant - Hydrophilic
CLASSIFICATION ON THE BASIS OF REMOVAL

## Slide 28
Method A: Water Washable
  Also called as self-emulsifying systems, can be removed from part by rinsing with water alone.
  These penetrants contain an emulsifying agent (detergent) that makes it possible to wash the penetrant from the part surface with water alone.
Method B: Post Emulsifiable - Lipophilic
  In this lipophilic systems, penetrant is oil soluble and interacts with oil-based emulsifier to make removal possible.
CLASSIFICATION ON THE BASIS OF REMOVAL

## Slide 29
Method C: Solvent Removable
  Solvent removable penetrants require the use of a solvent to remove the penetrant from the part.
Method D: Post Emulsifiable - Hydrophilic
  Post Emulsifiable - hydrophilic systems, used an emulsifier that is a water soluble detergent which lifts the excess penetrant from the surface of part with a water wash.
CLASSIFICATION ON THE BASIS OF REMOVAL

## Slide 30
Penetrants are also formulated to produce a variety of sensitivity levels.
The higher the sensitivity level, the smaller the defect that the penetrant system is capable of detecting.
The five sensitivity levels are:
  Level - Ultra Low Sensitivity
  Level 1 - Low Sensitivity
  Level 2 - Medium Sensitivity
  Level 3 - High Sensitivity
  Level 4 - Ultra-High Sensitivity
Classification of Penetrants on the basis of their Strength of Indication

## Slide 31
As the sensitivity level increases, so does the number of non-relevant indications.
Therefore, a penetrant needs to be selected that will find the defects of interest but not produce too many non-relevant indications.
Classification of Penetrants on the basis of their Strength of Indication

## Slide 32
  It's role is to pull the trapped penetrant material out of defects and spread it out on the surface of the part so it can be seen by an inspector.
  Developers also create a white background so there is a greater degree of contrast between the indication and the surrounding background.
Developer
  It should have good absorption characteristics.
  It should be chemically inert with test material.
  It should be able to uniformly cover the surface with thin smooth coating.
  It should provide a good contrast background for bright and clean indications
  It should be non-toxic.
  It should be easy to remove after inspection.
Characteristics of Good Developer

## Slide 33
  Developer classification is based on the method that the developer is applied.
  There are four forms of developers in general use:
    Water Soluble Developers
    Dry Powder Developers
    Water Suspendable Developers
    Non-aqueous Developers
Classification of Developers

## Slide 34
  They consist of a group of chemicals that are dissolved in water and form a developer layer when the water is evaporated away.
  The best method for applying water soluble developers is by spraying it on the part.
  Dipping, or brushing the solution on to the surface is sometimes used but these methods are less desirable.
Water Soluble Developers

## Slide 35
Dry powder developer is generally considered to be the least sensitive but it is inexpensive to use and easy to apply.
Dry developers are white, fluffy powder that can be applied to a thoroughly dry surface in a number of ways:
  Dipping parts in a container of developer.
  Using puffer to dust parts with developer.
  Using electrostatic powder spray guns.
  Placing part in a dust cabinet where developer is blown around and allowed to settle on the part.
Dry Powder Developer

## Slide 36
Dry Powder Developer
Advantage:
  When a dry developer is used, indications tend to stay bright and sharp since the penetrant has a limited amount of room to spread.
Limitation:
  Since dry powder developers only stick to the area where penetrant is present, the dry developer does not provide a uniform white background as the other forms of developers do.

## Slide 37
Water suspendable developers consist of insoluble developer particles suspended in water.
Water suspendable developers require frequent stirring or agitation to keep the particles from settling out of suspension.
Water suspendable developers are applied to parts in the same manner as water soluble developers.
Parts coated with a water suspendable developer must be forced dried just as parts coated with a water soluble developers are forced dried.
Water Suspendable Developers

## Slide 38
Non-aqueous developers suspend the developer in a volatile solvent and are typically applied with a spray gun.
Non-aqueous developers are commonly distributed in aerosol spray cans for portability.
Since the solvent is highly volatile, forced drying is not required.
Non-aqueous Developers

## Slide 39
Materials that are commonly inspected using DPT include the following:
  Metals (aluminum, copper, steel, titanium, etc.)
  Glass
  Many ceramic materials
  Rubber
  Plastics
Common Uses of Dye Penetrant Testing

## Slide 40
Sensitive to small surface discontinuities
Can inspect metal and non-metal
Works on complex geometric shapes
Portable
Affordable
Its relatively easy to use
ADVANTAGES

## Slide 41
Only sensitive to surface-breaking defects.
Surface must be clean properly.
Can not inspect porous metal generally.
No depth sizing.
Some rubber and plastics may be affected by penetrant material
LIMITATIONS

## Slide 42
  When proper health and safety precautions are followed, liquid penetrant inspection operations can be completed without any harm to inspection personnel.
  Some of the most common safety concerns are:
    Review material safety datasheet.
    Proper ventilation in confined spaces
    PPE’s should be worn to protect against skin irritation
    To protect injury to eyes, do not look directly inro UV light.
    Ignition sources to be avoided
Safety Precautions

## Slide 43
  Dye penetrant inspection is the one of the most widely used low cost inspection method.
  It can be used to locate all kinds of surface breaking flaws in all non-porous materials (metals, plastics, or ceramics).
  Penetrants are classified on the basis of their physical properties, removal techniques, and their strength of indication.
  Developers are classified on the basis of the method of their application.
  Proper health and safety precautions must be followed while performing this test.
Summary

## Slide 44
https://www.youtube.com/watch?v=DysflzHNy4Y&list=PLN_g_HrGTvQ0284U-3o8ugL98f8v6uE0-&index=8
https://www.youtube.com/watch?v=8I1onrUqjDA&ab_channel=NDTChannel
https://www.youtube.com/watch?v=8I1onrUqjDA
https://www.youtube.com/watch?v=1cl2ULh0_ss
https://www.youtube.com/watch?v=mIXIcR59dRE
https://www.youtube.com/watch?v=E8ebW1aNTyw
Reference Links

## Slide 45
  Thank You